“Surface Characterization of Bi2Te2.9Se0.1 single crystals”

Maunik Jani , Manisha Patel, S.M. Vyas, G.R. Pandya

Bi2Te2.9Se0.1 single crystals have been grown by the Bridgman technique with the freezing interface temperature gradient 650C/cm and growth velocity 0.5cm/hr. A parallel striations perpendicular to the ingot axis were observed on the top free surfaces of crystals, indicates layer growth mechanism is predominant among them.