Poly-CPDT films decorated with

dinuclear Re(I) complex chromophore pendants:

electrochemical and spectroscopic properties

Giuseppe D’Alfonso, Monica Panigati, Elsa Quartapelle Procopio,

Dip. di Chimica Inorganica, Metallorganica e Analitica, Univ. degli Studi di Milano,

Via Venezian 21, 20133 Milano, Italia,

giuseppe.dalfonso@unimi.it, monica.panigati@unimi.it

Francesco Sannicolò, Giovanni Rampinini,

Dipartimento di Chimica Organica e Industriale, Università degli Studi di Milano,

Via Venezian 21, 20133 Milano, Italia,

francesco.sannicolo@unimi.it

Valentina Bonometti, Patrizia Mussini

Dipartimento di Chimica Fisica ed Elettrochimica, Università degli Studi di Milano, Via Golgi 19, 20133 Milano, Italia

valentina.bonometti@unimi.it.

In our current development of new classes of luminescent dinuclear Re(I) complexes, looking for innovative hybrid materials for solid-state devices, we have synthesized and electrochemically characterized the compound Re2(CO)6(-H)(-3Me-pydz)(-OOC-cpdt), a novel conjugate between a luminescent complex and a cyclopentabithiophene (cpdt) unit. By comparison with the corresponding free dinuclear Re complex and with the free HOOCcpdt ligand the CV peaks of the new conjugate have been assigned to the different redox centers. Efficient and very regular electrochemical polymerization has been obtained on GC, Pt, and ITO electrodes as a consequence of the high polymerization ability and regioselectivity of the terminal (-thiophene positions of cpdt. The resulting films have been characterized by CV, EQCM, EIS and UV-vis spectroelectrochemistry. They are stable even upon repeated cycling, exhibiting two subsequent reversible oxidation peaks, whose relative charge ratio is regularly depending on the potential scan rate (possibly, on account of different rates of the counter ion ingress/egress). They also exhibit conspicuous charge trapping features, in terms of both quantity and stability, and excellent electrochromic properties.

# Text boxes

= Re(CO)3